Product Technical Datasheet

Version: V1.0

Revision Date: 2025-06-10

Basic Information

- Chemical Name：Ethyl 3-Ethoxypropionate

- Abbreviation：EEP

- CAS No.：763-69-9

- Molecula Formula：C6H12O3

- Molecular Weight：132.16g/mol

- Appearance：Colorless and transparent liquid with no visible impurities.

- Odor：It has a slight fruity or ether-like odor.

Physicochemical Indicators

| Item | Industrial Grade Standard |
| --- | --- |
| Purity (GC) | ≥99.0% |
| Acid Value (mgKOH/g) | ≤0.20 |
| Moisture Content (%) | ≤0.10 |
| Color (Pt-Co) | ≤15 Hazen |
| Density (25℃, g/mL) | 0.945±0.002 |
| Flash Point (closed cup, ℃) | ≥54 |
| Boiling Point (at Atmospheric Pressure, ℃) | 156-159 |
| Refractive Index (n₂₀^D) | 1.405-1.408 |

- Main Application Fields

- Coatings and Inks Industry:
As a high-boiling-point solvent, it is used in polyurethane coatings, acrylic coatings, amino baking varnishes, etc., to improve the leveling property and glossiness of the coating film, and reduce defects such as pinholes and orange peel;
It is applied in screen printing inks and gravure printing inks to enhance the adhesion of the ink to substrates (e.g., plastics, metals), and it has no pungent odor.

- Electronic Chemicals Field:
It is used in photoresist strippers and electronic cleaning agents, which can effectively dissolve photoresist residues and cause no corrosion to semiconductor substrates (such as silicon wafers and glass);
As a solvent for electronic packaging materials, it improves the uniformity and stability of packaging adhesives.

- Pharmaceuticals and Fine Chemicals:
As a pharmaceutical intermediate, it is used in the synthesis of antibacterial drugs and cardiovascular drugs;
In pesticide formulations, it acts as a solvent to enhance the stability and permeability of active ingredients.

- Other Fields
It serves as a solvent for cosmetic raw materials (such as nail polish and perfume), improving the product's skin feel and volatility;
In the adhesive industry, it is used in hot-melt adhesives and epoxy adhesives to adjust the curing speed and bonding strength.

Packaging Specifications

Industrial grade: 198kg iron drum

Precautions for Storage (and Use)

It should be stored in a cool, dry and well-ventilated place, away from ignition sources, heat sources and oxidizing agents (such as nitric acid, potassium permanganate); direct sunlight should be prevented, and the container should be kept sealed; the storage area should be equipped with leakage emergency treatment equipment and appropriate containment materials.

Shelf Life

From the date of production, when stored under specified storage conditions, the product can be kept sealed for 24 months. It needs to be re-inspected after expiration.

Precautions

When operating, wear goggles and chemical-resistant gloves to avoid direct skin contact.

The indicators and data provided in this manual are based on our current technical knowledge and practical experience. They are for reference only and do not constitute any guarantee. In view of the limitations of this product and the diversity of user requirements, please strictly test the adaptability of this product and the stability of the final product during use to verify whether it is suitable for your intended processes and applications and can achieve the predetermined objectives. You must also strictly comply with local safety, environmental protection regulations and operating specifications. The compiler of this manual shall not be liable for any losses caused by improper use or storage. The Technical Support and Customer Service Center of our company's Marketing Department is willing to provide you with consultation and application technical services related to the product. You are welcome to contact us by letter or phone.

Contact Address: No. 12 Taihe North Road, B1 District, Zhaoqing,China

Customer Service Center Hotline: +86(758)-2698552         Fax: +86(758)-2699551

http://www.zhidianchem.com                          E-mail：msd@zhidianchem.com