[image: image1.png]Dian Chi Chemical



[image: image1.png]                           

ZR5116 Technical Data Sheet

Product Name: ZR5116                       Version: V1.0
Chemical Name: Polyaspartic Ester Resin           Revision Date: 2025-06-10
Product Overview and Features
This product features high solid content (reaching up to 100%) and low viscosity, making it suitable for formulating environmentally friendly coatings;

It has high reactivity, with a surface drying time of only 5 minutes when reacting with NCO-ended curing agents, such as HDI trimer, thus improving production efficiency;

The coating film exhibits excellent flexibility, leveling properties, and gloss;

The paint film also demonstrates outstanding performance in weather resistance, water resistance, solvent resistance, acid and alkali resistance, salt spray resistance, etc.;

It has particularly prominent abrasion resistance [wear loss ≤20mg (500r/1000g)];
It has excellent adhesion to plastics such as ABS, PC, PVC, and various metals.
Product Applications

Used in the fields such as rapid-curing adhesives and bonding agents;

Can be used in protective coatings for heavy anti-corrosion fields such as steel structures and oil pipelines;

Used in fields such as road marking paints and concrete plugging materials;

Used in the Spray Polyurea Elastic Coatings (shortly SPUA) as a chain extender and main resin.
Performance Specifications

	Parameter
	Specification

	Relative Molecular Weight
	486

	Appearance
	Light yellow transparent liquid

	Solid Content / %
	97±2

	NH Equivalent (g/mol)
	Approximately 234

	Amine value (mg KOH/g)
	238 ~ 248

	Equivalent OH Content / %
	7.35 ~ 7.45

	Viscosity (mPa.s / 25℃)
	60~100

	Density/25℃
	1.05±0.02

	Flash Point / ℃
	approximately 97


Packaging Specifications
Iron Drum Packaging: 200 KG/drum, 25 KG/drum.
Storage and Usage Precautions
ZR5116 should be stored in a cool, dry, and well-ventilated area, away from ignition sources and heat. Prevent direct sunlight exposure, and keep the container sealed. The storage area should be equipped with emergency spill handling equipment and appropriate containment materials.
Shelf Life
When stored under the specified conditions, the product can be kept sealed for up to 12 months from the date of manufacture.

Notes

Coatings made with this product should ideally be cured for one week before testing their performance.
The specifications and data provided in this datasheet are based on our current technical knowledge and practical experience. They are for reference only and do not constitute a guarantee. Due to the limitations of resin functionality and the diversity of user requirements, please rigorously test the suitability and stability of this product for the intended process and use to ensure it meets the desired objectives. Our Marketing Department Technical Support and Customer Service Center are available to provide product consultation and application technical services. We welcome your inquiries by letter or phone.

Contact Address: No. 12 Taihe North Road, B1 District, Zhaoqing,China
Customer Service Center Hotline：+86(758)-2698552         Fax：+86(758)-2699551

http://www.zhidianchem.com                              E-mail：sales@zhidianchem.com
         GUANGDONG ZHIDIAN CHEMICAL CO., LTD.


