    [image: image1.png]Dian Chi Chemical



[image: image1.png]                           

ZR5210 Technical Data Sheet

Product Name: ZR5210                       Version: V1.3
Chemical Name: Polyaspartic Ester Resin           Revision Date: 2025-04-22
Product Overview and Features
This product is a solvent-free, high-solid, low-viscosity resin that can be formulated into environmentally friendly coatings with high solid content and low viscosity (application solids content up to 100%)；
It exhibits high reactivity and can react with NCO-ended curing agents, such as HDI trimer, achieving surface dryness in 15 minutes, thus enhancing production efficiency；
The coating film demonstrates excellent fullness, leveling properties, and gloss；
The coating film also possesses outstanding weather resistance, low-temperature flexibility, water resistance, solvent resistance, acid and alkali resistance, and salt spray resistance；
It has higher hardness with exceptional abrasion resistance [abrasion loss ≤ 20 mg (1000 cycles/1000 g)]；
Shows excellent adhesion to plastics such as ABS, PC, PVC, and various metals；
This product is highly compatible with most hydroxyl acrylic resins, CAB, and similar materials；
It reacts with elastic curing agents to produce elastic materials with excellent mechanical properties (elongation of 400%, tensile strength of 25 MPa) and can also react with NCO-ended hardener, such as HDI trimer (or dimer) to form rigid coatings；
Used as a Spray Polyurea Elastic Coating systems  (shortly SPUA) , serving as both a chain extender and a primary resin.
Product Applications

Applied in various high-end paints, such as automotive coatings and wood finishes, to enhance film fullness, gloss, hardness, and to accelerate drying；
Suitable for protective topcoats in heavy and light anti-corrosion fields, such as steel structures and oil pipelines；
Applicable in fields like foam landscape materials and concrete waterproofing materials；
Used in wind turbine blade coatings, including gel coats, putties, and topcoats for wind turbine blades.
Performance Specifications

	Parameter
	Specification

	Relative Molecular Weight
	554

	Appearance
	Light yellow transparent liquid

	Solid Content / %
	97±2

	NH Equivalent (g/mol)
	277

	Amine value (mg KOH/g)
	195-205

	Equivalent OH Content / %
	6.13~6.14

	Viscosity (mPa.s / 25℃)
	850-1800

	Density / 25℃
	1.06±0.02

	Flash Point / ℃
	90-95


Packaging Specifications
Iron Drum Packaging: 200 KG/drum, 25 KG/drum.
Storage and Usage Precautions
ZR5210 should be stored in a cool, dry, and well-ventilated area, away from ignition sources and heat. Prevent direct sunlight exposure, and keep the container sealed. The storage area should be equipped with emergency spill handling equipment and appropriate containment materials.
Shelf Life
When stored under the specified conditions, the product can be kept sealed for up to 12 months from the date of manufacture.

Notes

Coatings made with this product should ideally be cured for one week before testing their performance.
The specifications and data provided in this datasheet are based on our current technical knowledge and practical experience. They are for reference only and do not constitute a guarantee. Due to the limitations of resin functionality and the diversity of user requirements, please rigorously test the suitability and stability of this product for the intended process and use to ensure it meets the desired objectives. Our Marketing Department Technical Support and Customer Service Center are available to provide product consultation and application technical services. We welcome your inquiries by letter or phone.

Contact Address: No. 12 Taihe North Road, B1 District, Zhaoqing,China
Customer Service Center Hotline：+86(758)-2698552         Fax：+86(758)-2699551

http://www.zhidianchem.com                              E-mail：sales@zhidianchem.com
         GUANGDONG ZHIDIAN CHEMICAL CO., LTD.


