[image: image1.png]Dian Chi Chemical



[image: image1.png]                          

ZR5335 Technical Data Sheet

Product Name: ZR5335                       Version: V1.0
Chemical Name: Polyaspartic Ester Resin           Revision Date: 2025-09-28
Product Overview and Features
ZR5335 is a solvent-free resin, containing secondary amino groups, which can react with polyisocyanates to make various coatings.

Solvent-free with low viscosity. For the formulation of high-solid or solvent-free coatings.

Compared with ZR5210 and ZR5238, its reaction activity is adjustable between them, thus better toughness is available.

High reactivity. Touch dry in 20-30 minutes when react with NCO-ended curing agents, such as HDI Trimer to improve the production efficiency.

The coating film has excellent fullness, leveling performance and high gloss, excellent weather resistance, water resistance, solvent resistance, acid and alkali resistance, salt spray resistance and other properties. high hardness up to 2H and excellent abrasive resistance. 

Excellent adhesion with ABS, PC, PVC and other plastics and a variety of metals.

Has excellent compatibility with most of hydroxyl acrylic resin and CAB.

Product Applications

Can be used to make various high-grade pains, such as automobile paint, wood paint and so on. It can obviously improve the fullness, gloss and hardness and quicker drying time;

Can be used to make anti-corrosion coatings for steel structure, oil pipeline and other light or heavy anti-corrosion coatings;

Can be used for foam landscape, concrete waterproof materials and other fields;

Can be used to make wind blade coating field, such as gel coat, putty and topcoat;

Performance Specifications
	Parameter
	Specification

	Relative Molecular Weight
	667

	Appearance
	Light yellow transparent liquid

	Solid Content / %
	97±2

	NH Equivalent (g/mol)
	Approximately 334

	Amine value (mg KOH/g)
	155 ~ 180

	Equivalent OH Content / %
	5.0 ~ 5.2

	Viscosity (mPa.s / 25℃)
	1600 ~ 2800

	Density / 25℃
	1.02 ± 0.02


Packaging Specifications
Iron Drum Packaging: 200 KG/drum, 25 KG/drum.

Storage and Usage Precautions

ZR5335 should be stored in a cool, dry, and well-ventilated area, away from ignition sources and heat. Prevent direct sunlight exposure, and keep the container sealed. The storage area should be equipped with emergency spill handling equipment and appropriate containment materials.
Shelf Life
When stored under the specified conditions, the product can be kept sealed for up to 12 months from the date of manufacture.

Notes

Coatings made with this product should ideally be cured for one week before testing their performance.
The specifications and data provided in this datasheet are based on our current technical knowledge and practical experience. They are for reference only and do not constitute a guarantee. Due to the limitations of resin functionality and the diversity of user requirements, please rigorously test the suitability and stability of this product for the intended process and use to ensure it meets the desired objectives. Our Marketing Department Technical Support and Customer Service Center are available to provide product consultation and application technical services. We welcome your inquiries by letter or phone.

Contact Address: No. 12 Taihe North Road, B1 District, Zhaoqing,China
Customer Service Center Hotline：+86(758)-2698552         Fax：+86(758)-2699551

http://www.zhidianchem.com                              E-mail：sales@zhidianchem.com
         GUANGDONG ZHIDIAN CHEMICAL CO., LTD.


